## Slide 1
Cationic perylene dyes
Alafid F.1, Hrdina R.1, Burgert L.1, Bouška M.1, Pummerová M.2, Pištěková H.2, Sedlařík V. 2, Trousil V..3, Kubáč L.3, Vyňuchal J.4, Procházková Bára 5, Lovecká P.5
1 – Univerzita Pardubice, Fakulta chemicko-technologická.
2 – Univerzita Tomáše Bati ve Zlíně, Centrum polymerních systémů, Univerzitní institut.
3 – Centrum organické chemie s.r.o., Rybitví.
4 – Synthesia a.s., Pardubice.
5 – Vysoká škola chemicko-technologická v Praze.
fouzyramadanali.alafid@upce.cz

## Slide 2
Perylenebisimides (PBIs) has a significant photochemical and electrochemical stability [1]. PBIs show intense fluorescence and high electron mobility[2]. It has uses for such type of applications because of their structural which can be modifying PBI's imide and bay positions by alkyl chains and functional groups [3,4]. The cationic PTCDI derivative were synthesized as the fluorescent probe. Because of the planar aromatic structure of the structure, it has a capability to aggregate through aromatic π–π stacking interactions. However, since it contains two positive charges, repulsive interactions between the electrostatic charges decrease its tendency to aggregate. As a result, in aqueous solution at ambient temperature, the cationic compounds exists in equilibrium between the aggregated form and the free monomeric form.
------------------------------------------------------------------------------------------------------------------
(1) Tsai HY, Chen KY. 1,7-Diaminoperylene bisimides: synthesis, optical and electrochemical properties. Dyes
Pigments 2013;96:319-27.
(2) Dinçalp H, Kizilok S, Içli S. Fluorescent macromolecular perylene diimides containing pyrene or indole units
in bay positions. Dyes Pigments 2010;86: 32-41.
(3) Yue W, Jiang W, B€ockmann M, Doltsinis NL, Wang Z. Regioselective functionalization of corepersubstituted
perylene diimides. Chem Eur J 2014;20: 5209-13.
(4) Wicklein A, Kohn P, Ghazaryan L, Thurn-Albrecht T, Thelakkat M. Synthesis and structure elucidation of
discotic liquid crystalline perylene imide benzimidazole. Chem Commun 2010;46:2328-30.
Introduction

## Slide 3
Experimental part
These compounds were synthesized according to a published procedure with minor modification (Wei Ji, et al,. The Royal Society of Chemistry 2018, Analyst, 2018, 143, 1899–1905).
Compound 2
Compound 1
Figure 1.

## Slide 4
Yield of Compound 1: 90 % related to PDA.
Elemental analysis : Calculated for C36H38N4O4I2 : C, 50.13%, H, 4.54%, N, 6.63%, I, 30.05.
Found: C, 50.17%, H, 4.54%, N, 5.27%, I, 32.5.
HR-MALDI-MS (DHB): calcd for C36H38N4O4 m/z 590.28931 ([M-2I]2+), found 590.29067.
HR-MALDI-MS (DHB): calcd for C36H38N4O4I m/z 717.19377 ([M-I]+), found 717.19507.
The process resulted in primary crystals with an average value of 268.10-10 m (268 Å).
Figure 2: Compound 1.
Characterization: Compound 1

## Slide 5
Characterization: Compound 2
Yield of Compound 2: 93 % related to PDA.
Elemental analysis : calculated for C38H42N4O6Br2 :C, 56.31%; H, 5.22%; N, 6.91%; Br, 19.72%.
Found: C, 57.57%; H, 5.31%; N 7.02%; Br, 18.31%.
HR-MALDI-MS (DHB): calcd for C38H42N4O6 m/z 650.30989 ([M-2Br]+), found 650.31171.
HR-MALDI-MS (DHB): calcd for C38H42N4O6Br m/z 729.22822 ([M-Br]+), found 729.23059.
The process resulted in primary crystals with an average value of 155.10-10 m (155 Å).
Figure. 3: Compound 2.

## Slide 6
SEM
Compound 2
Compound 1
Figure.4

## Slide 7
Singlet oxygen measurement of Compound 1 and 2
Table.1 Singlet oxygen production expressed as τ1/2 (s)
Product | τ1/2 (s) | Φ
Compound 1 | 11,3 | 0,24
Compound 2 | 12,4 | 0,22
Loss of DPP using the submitted samples
Loss of sodium salicylate using the submitted samples
Both cationic perylenes have a high quantum yield and produce singlet oxygen in amounts slightly higher than chlorinated derivatives of perylene.
Figure 5.

## Slide 8
Differential scanning calorimetry (DSC) for PP granulate.
Fig. 6 DSC analysis, material granulate PP, second heating
The dominant component of the PP polymer (Tm = 164 °C) it is also present in small amounts PE-HD (peak with Tm around 120°C).
Figure.7 Samples after labeling: Polypropylene (left), Compound 1(middle ), Compound 2 (right).

## Slide 9
SEM.
Fig. 8 SEM PP images Polypropylene (left), Compound 1(middle ), Compound 2 (right).
Images of the fracture side of the samples show a homogeneous distribution of additives in the polypropylene matrix. The PP matrix itself appears to be additive with a tile-shaped particulate filler.

## Slide 10: Table 2. Results of antibacterial activity of PP samples against bacterial strain Staphylococcus aureus, E.coli and Candida albicans
 |  | Staphylococcus aureus |  |  | Escherichia coli |  |  | Candida albicans |  | 
 |  | N (CFU/cm2) | log N | R | N (CFU/cm2) | log N | R | N (CFU/cm2) | log N | R
PP (reference) | Shaken immediately | 8,2.103 | 3,9 | - | 4,4.104 | 4,7 | - | 1,0.103 | 3,0 | -
 | with exposure | 4,5.104 | 4,7 |  | 6,0.105 | 5,8 |  | 5,3.104 | 4,7 | 
 | in the dark | 9,3.104 | 4,9 |  | 7,3.105 | 5,9 |  | 6,4.104 | 4,8 | 
PP + Compound 1 | with exposure | 1,6.104 | 4,2 | 0,5 | 3,0.105 | 5,5 | 0,3 | 9,2.103 | 4,0 | 0,7
 | in the dark | 9,4.104 | 4,9 | 0 | 3,1.105 | 5,5 | 0,4 | 7,2.103 | 3,9 | 0,9
PP + Compound 2 | with exposure | 4,1.103 | 3,6 | 1,1 | 2,7.105 | 5,4 | 0,4 | 9,5.101 | 2,0 | 2,7
 | in the dark | 1,4.104 | 4,2 | 0,7 | 3,7.105 | 5,7 | 0,2 | 1,5.103 | 3,2 | 1,6
Antibacterial activity

## Slide 11: Antibacterial activity
Sample |  | S. aureus CCM 4516 | 
 |  | c (CFU/ml) | log c
1 - 100% cotton MILETA, reference | Shaken immediately | 1,2.104 | 4,1
 | Incubated with exposure | 1,5.103 | 3,2
 | Incubated in the dark | 1,5.105 | 5,2
2 – 100% cotton + compound 1, st. coloring 3 %, wt. XENOTEST 1, 3 %, Compound 1 | Shaken immediately | 8,9.102 | 2,9
 | Incubated with exposure | < 1 | 0
 | Incubated in the dark | 3,0.100 | 0,5
3 - 100% cotton + compound 1, st. Coloring 5 %, wt. XENOTEST 2, 5 %, Compound 1 | Shaken immediately | 2,2.103 | 3,3
 | Incubated with exposure | < 1 | 0
 | Incubated in the dark | 1,0.100 | 0
4 - 100% cotton + compound 2, st. coloring 3 %, wt. XENOTEST 3, 3 Compound 2 | Shaken immediately | 2,2.103 | 3,3
 | Incubated with exposure | < 1 | 0
 | Incubated in the dark | 2,5.100 | 0,3
5 - 100% cotton + compound 2, st. Coloring 5 %, wt. XENOTEST 4, 5 %, Compound 2 | Shaken immediately | 2,7.104 | 4,4
 | Incubated with exposure | < 1 | 0
 | Incubated in the dark | < 1 | 0
Table 3. Results of the concentration of viable bacteria and the values of antibacterial activity (A) against growth Staphylococcus aureus

## Slide 12
Application
Figure.9 Compound 1, Color fastness to washing at 60 °C according to ČSN EN ISO 105 - C06 (800 120). Dyed material: 100% cotton.

## Slide 13: Table 4. Color shade and color change
Color shade 1% - color change | Staining cotton | Staining wool
4 – 5 R | 3 – 4 | 3
Color shade 2.5% - color change | Staining cotton | Staining wool
4 – 5 R | 3 | 3
Color shade 5% - color change | Staining cotton | Staining wool
4 – 5 R | 3 – 4 | 3

## Slide 14
Figure.10 Wash fastness at 40°C( left) and 60° C (right) - ČSN EN ISO 105 – C06 (800 120). Dyed material :100% cotton.

## Slide 15
Wash fastness 40°C | Staining cotton | Staining wool
Color shade 3 % - color change 4 – 5 R | 4 | 4
Color shade 5 % - color change 4 – 5 R | 4 | 3 - 4
Wash fastness 60°C | Staining cotton | Staining wool
Color shade 3 % - color change 4 – 5 R | 3 | 2 - 3
Color shade 5 % - color change 4 – 5 R | 3 | 2
Table 5. Wash fastness 40°C, and at 60°C

## Slide 16
LIGHTFASTNESS – XENOTEST (ISO 105-B02).
Sample | Lightfastness XENOTEST
Compound 1 Color shade 3% | 3
Compound 1 Color shade 5% | 3
Compound 2 Color shade 3% | 3
Compound 2 Color shade 5% | 3
Table. 6 Lightfastness
Figure.11 Dyed material: 100% cotton. Evaluated immediately after the xenostest.

## Slide 17
If the samples are stored in the dark after the xenotest, the coloration will return to this level in a few days which mean it is photochromic dye:
Figure.12: Immediately after the xenostest (on the left), after 14 days in dark (on the right).

## Slide 18
This work was supported by the grant TRIO program, Ministry of Industry and Trade, Czech Republic, project MPO TRIO FV30048.
Acknowledgements

## Slide 19
Thank You For Your Attention